## Slide 1
A new control parameter for the glass transition of glycerol.
D. L’Hôte, R. Tourbot, F. Ladieu, P. Gadige
Service de Physique de l’Etat Condensé (CNRS, MIPPU/ URA 2464), DSM/IRAMIS/SPEC/SPHYNX CEA Saclay, France
Main Funding:
Additionnal Funding:

## Slide 2
The most emblematic claim of this work :
Small effect: discovered through a nonlinear technique
 The most interesting is not dTg but what we learn when varying P, Est.
 Previously, the unique way to change Tg was the Pressure P
 Est is a new control parameter in Glycerol.

## Slide 3
Outline:
Motivations for nonlinear experiments
II) Our specially designed experiment
III) Results on Glycerol
    Order of magnitude and comparison to the Box model
    Relation to Ncorr
    Tg shift
IV) Some naives questions/ideas.
Summary and Perspectives.

## Slide 4
How to combine the existence of correlations with the absence of order ?
12
10
8
6
4
2
0
-2
-4
Tg / T
Log (viscosity)  ta
Angell, Science 267 (1995)
Tg / T
0 0.2 0.4 0.6 0.8 1.0
Ea  when T 
 Correlations  when T 
No (static) cristalline order
S(q) [a.u.]
Polybutadiene, Tg 180K
What happens around Tg ???
Relaxation time ta
tα
tα~ 10-12s
T
Tm
Tg
Liquid
Supercooled
liquid
Glass
ta=100s
(Crystal)

## Slide 5
Dynamical Heterogeneities in supercooled liquids
Ncorr = average number of dynamically correlated molecules :
Hurley, Harowell, PRE, 52, 1694, (1995)
… directly observed in granular matter or in numerical simulations.
Example : numerical simulations on soft spheres :
…Experimentally, the heterogeneous nature of the dynamics has been established through various breakthroughs:
NMR experiments
Local measurements
Tracht et al. PRL81, 2727 (98),
J. Magn. Res. 140 460 (99),…
E. Vidal Russell and N.E. Israeloff , Nature 408, 695 (2000).
« clusters » of 30-90 monomers
When T: Ncorr would , which would explain why ta increases so much
 Hole burning experiments

## Slide 6
Dynamical Heterogeneities and NHB.
Non Res Hole Burning: supercooled dynamics IS heterogeneous (at least in time)
e.g. R.Richert’s group: PRL, 97, 095703 (2006); PRB 75, 064302 (2007); EPJB, 66, 217, (2008); PRL, 104, 085702, (2010)…
A distribution of t’s exists
e(t,w) : should be globally shifted in w
 Many improvements since Schiener, Böhmer, Loidl, Chamberlin Science, 274, 752, (1996)
 The central idea in Schiener et al ’s seminal paper in 1996:
… Can nonlinear experiments give MORE than originally expected ??....
Strong field (V0) at W
No distribution of t
e(t,w) : should be mainly modified close to W

## Slide 7
The prediction of Bouchaud-Biroli (B&B): PRB 72, 064204 (2005)
Natural scale of c3
cs= static value of cLin
a3= molecular volume
H
wta
« 1 »
Ncorr= number of dynamic. correlated molec.
ta (T) : typical relaxation time
H: scaling function
Systematic c3(w,T) measurements to test the prediction and possibly get Ncorr(T)
AND
Ncorr « large enough »

## Slide 8
The issue of interpretations : Box Model versus B&B
c3(w,T) : Ncorr(T) or not ?
→ Each DH « k » has a Debye dynamics.
{tk} chosen to recover clin(w) at each given T.
Box model assumptions (designed for NHB):
→ Applying E: each DH « k » is heated by dTk (ttherm) with ttherm  tk.
as{tk}ta heat diffusion over one DH takes a macroscopic time close to Tg.
c3 does NOT contain Ncorr (Box model is space free)
c3
wta
« 1 »
For a pure ac field Eac cos(wt): w and T dependences are qualitatively similar in the Box model and in B&B

## Slide 9
Some experiments done since B&B’s prediction (2005)
Using Est will shed a new light on this interpretation issue
→ Very good fits at 1w (better than at 3w)
Box model :
B&B:
e.g. R.Richert’s group: PRL, 97, 095703 (2006); PRB 75, 064302 (2007); EPJB, 66, 217, (2008); PRL, 104, 085702, (2010)…
Our group: PhD’s of C. Thibierge and C. Brun. PRL (2010); (2012) PRB (2011) (2012); JChem Phys (2011) ,
→ Accounts for the transient regime at 1w
→ Several liquids tested (Richert PRL (2007))
Augsburg group: PhD of Th. Bauer : 2 PRL’s in (2013); etc…
→ Test of B&B’s prediction: OK
→ Evolution of Ncorr(T) or of Ncorr(ta)
→ Several liquids tested (Lunkenheimer & Loidl)

## Slide 10
Outline:
Motivations for nonlinear experiments
II) Our specially designed experiment
III) Results on Glycerol
    Order of magnitude and comparison to the Box model
    Relation to Ncorr
    Tg shift
IV) Some naives questions/ideas.
Summary and Perspectives.

## Slide 11
Linear term
First non-linear term
 Specially designed setup
Dielectric setup and orders of magnitude
P
e
Supercooled liquid, controlled T
VS (t)
For “low enough” E

## Slide 12
Our setup to measure cubic susceptibilities
Vmeas
r1
Z2 = thick
capacitor
(2×thin)
Z1 = thin
capacitor
r2
Vac e j w t + Vst
Bridge with two glycerol-filled capacitors of different thicknesses
C. Thibierge et al, RSI 79, 103905 (2008))
DV~ Vst2 Vac
Phase (DV) = cte
 when r1Z1=r2Z2 : Plin cancels
ILin +
INonlLin
2 ILin +
8 INonlLin
DV = Vmeas(Vac,Vst)
- Vmeas(Vac,0)
gives PNonLin

## Slide 13
Outline:
Motivations for nonlinear experiments
Our specially designed experiment
III) Results on Glycerol
    Order of magnitude and comparison to the Box model
    Relation to Ncorr
    Tg shift
IV) Some naives questions/ideas.
Summary and Perspectives.
 NB:
wta  f/fa
fa peak of clin’’(w)
|clin(w)| has no peak

## Slide 14
At constant T:
 humped shape for |c2;1(1)|
 maximum happens in the range of fa
Scaling of the hump in T
Main features of
Same qualitative trends as for c3(1) and c3(3)

## Slide 15
Comparing and
For the first time, Box Model is unable to account for a cubic response:
Decisive point for the interpretation issue …
 Compare |c3(1)|/4 and |c2;1(1)|
→ Same order of magitude
, [m²/V²]
→ Measurements (  ) are in the stationnary regime (tst>> ta)
Est
tst
t
Varying Est  ZERO dissipated power
Box model’s prediction :|c2;1(1)|<< |c3(1)|
Box model’s prediction is too small by a factor 300 for |c2;1(1)|
(ions)

## Slide 16
Outline:
Motivations for nonlinear experiments
Our specially designed experiment
III) Results on Glycerol
    Order of magnitude and comparison to the Box model
    Relation to Ncorr
    Tg shift
IV) Some naives questions/ideas.
Summary and Perspectives.

## Slide 17
Comparing the w dependences of and of
Direct link with
Berthier et al., Science (2005); JCP, (2007); PRE (2007).
 For f/fa > 0.2:
with
expected from
for both Re and Im parts
 T
 For f/fa < 0.2: “Trivial” dominates
Reshuffling  Ideal gas at t >>ta

218K
197K

## Slide 18
T-dependences of the dimensionless nonlinear suscept.
is T-independent in the trivial limit (ideal gas)
if B&B’s prediction holds
 “Trivial”
looks OK
 Similar T dependences for
w and T dependences consistent with X2;1(1) ~ Ncorr (OK within MCT)

## Slide 19
Each Dyn.Het.  µ = µm
Can we fit nonlinear resp. ? The ‘‘toy model’’ as an attempt :
//z
Simplest example: D=0=q1
can it fit the data ? …
Two key points
 Amorphous Order («as» in S.G.)
Crossover to trivial is enforced at f<<fa
in a double well (to get long t),
of assymetry D

## Slide 20
Fits at Tg+17K:
 Ncorr has the right order of magnitude
 good fits for ALL the Xn(k)
 … but with different values of Ncorr (toy model)
Ncorr=10
d=0.60
Ncorr=15
d=0.60
Ladieu, Brun, L’Hôte, PRB 85, 184207, (2012)
L’Hôte, Tourbot, Ladieu, Gadige to appear in PRB (2014)

## Slide 21
Outline:
Motivations for nonlinear experiments
Our specially designed experiment
III) Results on Glycerol
    Order of magnitude and comparison to the Box model
    Relation to Ncorr
    Tg shift
IV) Some naives questions/ideas.
Summary and Perspectives.

## Slide 22
Hensel-Bielowka et al. , PRE (2004)
Translating c2,1(1) as a dTg shift
Pressure experiments:
dTg(P) is drawn from :
Slight trivial distortion of c2,1(1) l≠1
Same method for Est:
dTg=3kEst2  Est is a new control parameter in glycerol

## Slide 23
A picture: D.H.  overcrowded subway
Density … S  and ta
Increasing Est …
Est … S  and ta
Increasing Pressure …
Ncorr

## Slide 24
Outline:
Motivations for nonlinear experiments
Our specially designed experiment
III) Results on Glycerol
    Order of magnitude and comparison to the Box model
    Relation to Ncorr
    Tg shift
IV) Some naives questions/ideas.
Summary and Perspectives.

## Slide 25
Does TK follow Tg ?
 We find dTg (Est) > 0
|Est |
T
TK
Tg
« true » glass
« Supercooled liquid »
|Hst |
Tc
Spin Glass
Paramagnet
 S.G: dTg (Hst) < 0 or “very negative”
Is it allowed that dTK(Est)>0 ?  e.g. peculiarity of 1RSB ?
T
 Est slows down the dynamics
 S.G.: Hst speeds up the relaxation
Not a contradiction since T>Tg differs from T<Tc
Y.G. Joh et al, PRL 82, 438 (1999)
and Saclay data

## Slide 26
Can we test theories with cubic responses?
L. Levy et T. Oglieksi PRL57, 3288 (1986), L. Lévy, PRB, 38, 4963 (1988)
c3 (a.u.)
Ncorr [a.u.]
Above Tg
Too narrow to test theories relating ta and Ncorr
Quench at Tg-7K
In Spin Glasses: critical behavior nicely evidenced
Ncorr /Ncorr(eq)
ta, [s]
Brun et al. PRL109, 175702 (2012)
Brun et al. PRB 84, 104204 (2011)
ta, [s]
Quasi equilibrium

## Slide 27
Can we test theories with cubic responses?
AND
We can test theories
Ncorr [a.u.]
Above Tg
Brun et al. PRB 84, 104204 (2011)
ta, [s]
Ncorr [a.u.]
ta, [s]
Brun et al. PRL109, 175702 (2012)
Consistent with RFOT
NB: yields z>20 : not reasonnable
Consistent with Cammarota et al, JCP (2009)
Below Tg

## Slide 28
Recent works on cubic responses
How to choose a good model ?
A model accounting for c3 will ALSO capture dyn. spatial aspects ☺
→ In colloids: experiments and MCT done for oscillatory shear :
 See Brader et al, PRE, 82, 061401, (2010)
 MCT for oscillatory stress is coming: see Matthias Fuchs papers (Konstanz univ.)
t / ta
1
→ In supercooled liquids:
 Bouchaud Biroli PRB 72, 064204 (2005) and Tarzia et al, JCP (2010) in MCT
G. Diezemann : PRE, (2012); JCP(2013); arXiv: 1407.4333v1
  no general link between c3 and four times correlation functions (trap models…)
  This link depends on the chosen model and chosen observable.
AND crossover to trivial
with
Why not simulate ? (d=3)